## Slide 1: K-Ont Template Generation
Knowledge-guided crystal structure prediction for battery cathodes
Team 25 · Knowledge-Driven Representation and Analysis of Battery Cathode Materials
Guide: Dr. Gowtham R · Co-guide: Dr. M. Ulaganathan · Amrita Vishwa Vidyapeetham, Coimbatore
Notes: This deck explains the method that gave our best structure-generation results: K-Ont template generation. In one sentence: most new materials reuse an atomic arrangement that already exists in a known material, so instead of asking a language model to invent the whole crystal, we use our knowledge graph and the K-Ont encoder to find the right known arrangement and put the new elements into it. I will go through the problem, the architecture, each component, the workflow for one new composition, the results, and what did not work.

## Slide 2: The problem: predicting a crystal from its composition
Language-model generation (CrystaLLM)
Writes the crystal as CIF text, token by token: space group, cell, then every atom position. It must get every coordinate right, and often picks the wrong arrangement.
Knowledge idea: reuse a known framework
Most new materials share an atomic arrangement (framework) with a known one, e.g. NaFePO₄ and LiFePO₄ are both olivine. Find that material in the knowledge graph and place the new elements into its framework.
48.3%
CrystaLLM: right structure at the first attempt (902 held-out materials)
85.6%
of held-out materials have a correct framework already in our knowledge graph
90.9%
with the extended graph (+5,267 Materials Project materials)
Notes: CrystaLLM is a GPT model that writes a crystal file as text. It decides the space group, the cell and every atom coordinate itself. On our 902 held-out materials, its first sample is right 48.3% of the time. The key observation is that for 85.6% of those materials, some material in our knowledge graph already has the right framework, and 90.9% with the extended graph. So the knowledge to solve most cases is already there; the question is how to find and use it.

## Slide 3: Architecture: K-Ont template generation
1 OFFLINE, ONCE
battGPT ontology
classes, axioms, families
Knowledge graph
5,000 materials (MP)
Verbalizer
material → text
K-Ont training
ontology + materials in one hyperbolic space
Framework retrieval
“has the framework of” + retention
K-Ont retriever
one model
Template pool
known structures
2 PER COMPOSITION
New composition
e.g. NaMnPO₄
Same-pattern candidates
ABCD₄ → LiFePO₄, …
Structure-free description
formula, elements, chemistry
Rank frameworks
K-Ont similarity + ranker → top 3
Element substitution
3 template structures
CrystaLLM
5 samples
CHGNet relaxation
lowest energy of 8 wins
Predicted structure
one CIF
60.5%
right at the 1st attempt (CrystaLLM 48.3%)
77.3%
right within 8 attempts (CrystaLLM 68.3%)
69.3%
one committed answer (CrystaLLM 63.7%)
32 / 34
novel cathodes confirmed more stable
Notes: This is the whole system on one slide. The top band is done once, offline. The battGPT ontology and the knowledge graph of 5,000 Materials Project materials are turned into text by the verbalizer and used to train K-Ont, which places ontology concepts and individual materials in one hyperbolic space. K-Ont is then taught one more relation, 'has the framework of', with a retention step so it keeps everything else; the result is one retriever model. The knowledge graph's materials with known structures form the template pool. The bottom band runs for every new composition: candidates with the same formula pattern come from the pool, K-Ont ranks them against the new composition's structure-free description, the top 3 frameworks receive the new elements, CrystaLLM adds 5 samples, and CHGNet relaxes all 8 and keeps the lowest-energy structure. The numbers at the bottom are the headline results.

## Slide 4: Component 1: battGPT, the knowledge source
OWL 2 DL ontology extending EMMO and BattINFO (the European materials and battery ontologies)
Extension I, crystallography: crystal structure, unit cell, space group, sites, species, bonds, DFT properties
Extension II, structure families: layered oxide, spinel, rock salt, olivine, NASICON, garnet, perovskite, LGPS, argyrodite
Population pipeline: Materials Project → pymatgen analysis → RDF knowledge graph, checked with the ELK and HermiT reasoners
5,000
Li/Na materials, each with its known crystal structure
5.6 M
triples in the knowledge graph
9
disjoint structure-family classes
+5,267
materials in the extended template pool
Notes: battGPT is our ontology and knowledge graph. The ontology adds two things EMMO lacks for crystal generation: a crystallography model and a structure-family vocabulary. The pipeline fills it with 5,000 lithium and sodium materials from Materials Project, each with its real crystal structure. For template generation, the knowledge graph plays two roles: it is what K-Ont learns from, and its materials are the pool of known frameworks we can reuse. Adding 5,267 more materials raised the share of targets with a correct framework available from 85.6% to 90.9%.

## Slide 5: Component 2: the K-Ont encoder
general concepts near the centre · families further out · individual materials (open circles) near the edge
Axiom rows (from the ontology)
C ⊑ D, e.g. olivine ⊑ polyanion family; existential restrictions via role rotations
Typing rows (from the knowledge graph)
each material's text description ⊑ its class, e.g. ⊑ substance
Relation rows (from the knowledge graph)
material ⊑ ∃ has structure . crystal, with in-batch negatives
Held-out typing: 1.000 with the ontology's axioms vs 0.641 without; hierarchy MRR 0.969 vs 0.313. The ontology is what gives K-Ont its type reasoning.
Notes: OnT, published at ISWC 2025, embeds the names of ontology concepts in a Poincaré ball, a hyperbolic space where distance from the centre encodes depth in the hierarchy. OnT cannot embed individual materials. K-Ont keeps OnT's model and loss, and adds the knowledge graph: every material is written as a short text description and trained together with three kinds of rows: the ontology's axioms, typing rows saying which class a material belongs to, and relation rows linking a material to its crystal. On 1,018 held-out materials it types materials perfectly; without the ontology's axioms typing drops to 64%, so the ontology matters.

## Slide 6: Component 3: teaching K-Ont to find frameworks
Query
a material's description WITHOUT its structure: formula, elements, chemistry (all a new composition has)
has the framework of
new relation learned by K-Ont
Answer
the FULL description (with space group, lattice, sites) of a known material sharing its framework
Problem: catastrophic forgetting
Learning the new relation alone erased K-Ont's typing of materials and crystals.
Fix: retention (one model, K-Ont-52c)
Keep the original embeddings of all knowledge-graph sentences, 20,000 GALEN concepts and 23 relation phrases while learning. Typing, families and GALEN are kept; stable over 3 seeds.
Training uses only K-Ont's training materials; the 902 test materials and their candidates are never seen.
Notes: To retrieve templates, K-Ont learns one extra relation, 'has the framework of'. The query side is what we know about a new composition: its description without any structure lines. The answer side is the full description of a known material that shares its framework, meaning the same formula pattern and space group. Learning this alone made K-Ont forget its typing, the classic catastrophic forgetting problem. Our fix is a retention loss that keeps the original embeddings of the knowledge-graph sentences, the GALEN ontology concepts and the relation phrases. The result is a single model that still does all the ontology checks and also retrieves frameworks, and it is stable across three random seeds.

## Slide 7: Workflow for one new composition
1
Find candidates
KG materials with the same formula pattern (anonymous formula), different formula
2
Rank with K-Ont
score each candidate against the composition's structure-free description; a ranker adds KG facts; keep top 3
3
Substitute elements
place the new elements on each framework's sites; scale the cell → 3 template structures
4
Add CrystaLLM samples
the language model writes 5 more candidates for frameworks the graph may lack
5
Relax and pick
CHGNet relaxes all 8 candidates; the lowest energy per atom is the answer
Example: NaMnPO₄ (illustration)
1 pattern ABCD₄ → LiFePO₄, LiMnPO₄, LiCoPO₄, …
2 K-Ont scores every candidate; the top 3 frameworks are kept
3 Na → Li site, Mn → Fe site, P → P, O → O; cell scaled to the new ions
4 CrystaLLM writes 5 structures from the composition alone
5 CHGNet keeps the most stable of the 8
Notes: Here is the workflow step by step. One: collect knowledge-graph materials whose formula has the same pattern; NaMnPO4 has the pattern ABCD4, so LiFePO4 and similar phosphates qualify. Two: K-Ont encodes the new composition's structure-free description and scores every candidate; a gradient-boosted ranker combines this with knowledge-graph facts such as how common a framework is, and we keep the top three. Three: put the new elements onto each framework's sites, which takes milliseconds. Four: CrystaLLM writes five more candidates, which covers frameworks the graph does not contain. Five: CHGNet, a machine-learned force field, relaxes all eight and we keep the lowest-energy one. The example on the right is an illustration of the steps, not a reported result.

## Slide 8: Inside step 3: element substitution
Elements are matched by amount in the formula, then by electronegativity, so ions of similar character share a site
The cell is scaled by the ratio of atomic sizes, a first guess at the new volume
CHGNet relaxation then corrects atom positions and the cell shape
Stoichiometry stays exact: only elements with the same count can swap
Template LiFePO₄ | → | Target NaMnPO₄
Li (1 per formula) | → | Na
Fe (1) | → | Mn
P (1) | → | P
O (4) | → | O
Tested: oxidation-state aware placement (bond valence + ionic radii)
Only 556 of 6,553 placements change, and accuracy stays the same (60.3% vs 60.5% at the first attempt). The simple rule is already chemically consistent; errors come from wrong frameworks, not wrong sites.
Notes: A common question is whether simply swapping elements is chemically sound. The rule matches elements by how many times they appear in the formula and then by electronegativity, so for LiFePO4 to NaMnPO4, sodium takes lithium's site and manganese takes iron's. The cell is scaled by atomic size and then CHGNet relaxes the positions and cell. We also built a stricter version that reads each atom's oxidation state from the template's bonding and matches charges and ionic radii. It changed only 556 of 6,553 placements and did not change accuracy, which shows the simple rule is already chemically consistent. The remaining errors come from choosing the wrong framework.

## Slide 9: Why combine templates with CrystaLLM
Templates fail when…
the right framework is not in the graph (about 9% of targets), or elements land on the wrong sites
CrystaLLM fails when…
it invents the wrong framework or misplaces atoms while writing coordinates
Together…
they catch different materials; a physics-based energy pick chooses among them
System (8-candidate budget) | One final answer | Any of 8 right
Templates only | 61.7% | 71.4%
CrystaLLM only (8 samples) | 63.7% | 68.3%
3 templates + 5 CrystaLLM | 69.3% | 77.3%
8 candidates matches the “CrystaLLM × 8” baseline, so both systems get the same budget. The system still outputs one structure.
Notes: Neither method alone is best because they fail on different materials. Templates fail when the graph lacks the right framework; CrystaLLM fails when it invents the wrong one. Combined, any of the eight candidates is right 77.3% of the time, and the CHGNet pick gives one final answer that is right 69.3% of the time, against 63.7% for CrystaLLM choosing among its own eight samples. We use eight candidates so that the comparison with CrystaLLM times eight is fair.

## Slide 10: Results on 902 held-out materials
Chart: Right structure at the first attempt (%)
| CrystaLLM (fine-tuned) | Composition rule | Hautier substitution | K-Ont templates
Baselines | 48.3 | 51.3 | 52.1
K-Ont | 60.5
+12.2 pts
over CrystaLLM at the first attempt [9.0, 15.4]
77.3%
right within 8 attempts with CrystaLLM (vs 68.3%) [+6.9, +11.1]
69.3%
one committed answer by CHGNet (vs 63.7%) [+1.3, +9.7]
Brackets: 95% bootstrap intervals of the difference. Materials never seen in training.
Notes: These are the main numbers on 902 held-out materials whose true structures we know. K-Ont templates are right at the first attempt 60.5% of the time, against 48.3% for fine-tuned CrystaLLM, 52.1% for the standard Hautier substitution method and 51.3% for a simple composition rule. Combined with CrystaLLM, some candidate is right 77.3% of the time, and the single answer is right 69.3% of the time. All differences shown are statistically significant.

## Slide 11: Novel cathodes: 199 compositions not in Materials Project
34 / 0
compositions where adding K-Ont templates found a lower / higher energy structure than CrystaLLM-large alone
32 of 34
confirmed more stable by an independent energy-above-hull calculation
0.025 eV
median energy above hull of the templates (CrystaLLM-large: 0.087 eV/atom)
Energy above hull, 34 compositions | CrystaLLM-large | K-Ont template
Within 50 meV/atom of the hull | 13 | 23
Within 100 meV/atom of the hull | 19 | 27
Caveat: the 34 were selected because CHGNet favoured the template, so this confirms the ranking; a random sample is needed for an overall win rate.
Notes: For genuinely new compositions there is no true structure to compare against, so we compare stability. On 199 new cathode compositions, adding K-Ont templates to CrystaLLM-large found a lower-energy structure for 34 compositions and never a higher one. A teammate's independent energy-above-hull calculation confirmed the template was more stable in 32 of those 34, with a median of 0.025 eV/atom against 0.087. The honest caveat is that these 34 were chosen because CHGNet already preferred the template.

## Slide 12: What did not work: putting the knowledge inside CrystaLLM
Approach | Result
Soft prompt + gated adapters (K-Ont embedding of a retrieved analogue) | steers the framework, but at most +1.5 points
Ceiling: give CrystaLLM the TRUE analogue | only +2.1 (CrystaLLM), +2.7 (GPT trained without test materials)
Hard prompt: template's space group and cell as the prompt | 45.9%, worse than the template itself (60.5%)
Template editor: CrystaLLM rewrites the template | 22.1%; breaks correct templates
K-Ont checker re-ranks CrystaLLM's samples | +2.3 to +3.5 at the first sample; no gain after the CHGNet pick
Lesson
Knowledge tells the model which framework to use, but the model still has to write every atom position, and that is where it fails. Knowledge helps most when the retrieved structure is used directly.
Notes: Our original plan was to inject ontology knowledge into CrystaLLM. We built several versions and measured each against controls. The decisive test was the ceiling: even when we give CrystaLLM the true analogue, accuracy rises by only about two points, because the model still writes every coordinate itself. So the knowledge is most valuable when it enters as a ready structure, which is exactly what the template method does. This is a measured finding, not a failure of effort.

## Slide 13: Limitations and next steps
Limitations
A plain text encoder trained on the same graph relation picks templates about as well; K-Ont's distinct value is one model that also reasons over the ontology
Templates cannot create frameworks missing from the graph (~9% of targets)
No templates yet for systems with more than five elements
Energy pick uses CHGNet with a short relaxation
Novel-cathode check covers a CHGNet-selected subset
Next steps
Feed knowledge-track structures into the oxidation-state aware MatterGen screening funnel (MatterSim → stable, unique, novel → DFT)
Unbiased DFT sample of the novel cathodes
Mixed-site templates for 6–7 element systems
Property prediction (voltage, capacity) from K-Ont embeddings
Competency questions as SPARQL queries over the graph
Notes: The main limitation to be open about is that a plain encoder trained on the same relation ranks templates about as well as K-Ont, so K-Ont's contribution is doing this inside a single model that also understands the battery ontology. Templates also cannot invent new frameworks, and we have no templates yet for systems with more than five elements. Next, we plan to send these structures through the same MatterSim, stable-unique-novel and DFT screening used by the MatterGen track, get an unbiased DFT sample, and test K-Ont embeddings for predicting voltage and capacity.